Supplementary Information:

Epsilon-Fe2O3 is a novel intermediate for magnetite biosynthesis in magnetotactic bacteria

Tong Wen1, 3, †, Yunpeng Zhang1, 4†, Yuanyuan Geng1, Junquan Liu1, Abdul Basit1, Jiesheng Tian1, Ying Li1, Jilun Li1, Jing Ju2*, Wei Jiang1*

Supplementary Information Figure S1. HRTEM images with high resolution and the corresponding FFT analyses of intracellular iron oxide nanoparticles in MSR-1 wild type after the induction of ferric citrate for different time interval.

Supplementary Information Figure S2. Some representative HRTEM images of epsilon-Fe2O3 and alpha-Fe2O3 used for the phase ratio determination in Fig. 5 of the main text.

Supplementary Information Table S1. Crystallographic information of the -Fe2O3 exhibited in Figure 3a, Figure 4 and the theoretical data of -Fe2O3 and Fe3O4 (magnetite). For further crystallographic information, people can refer to pdf card as 33-0664 for -Fe2O3, 65-3107 for magnetite and 52-1449 for -Fe2O3, respectively.

| Image identifier | 5 min | 10 min | 15 min | 25 min |
| --- | --- | --- | --- | --- |
| Axis of projection, as indicated in Fig. 2 for epsilon-Fe2O3 | [-332] | [-332] | [-10 4 1] | [10 -8 3] |
| Reflections identified for epsilon-Fe2O3 | 110 and 1-13 | 110 and 1-13 | 122 and 13-2 | 21-4 and 122 |
| Possible axis of projection for magnetite | [03-1] | [03-1] | [4 1 -1] | [4 1 -1] |
| Possible reflections identified for magnetite | 200* and 113 | 200* and 113 | 022 and 1-13 | 1-31 and 115 |
| Ratio measured between two sets of reciprocal spacings (referred to as r1 and r2) | 1.68 r1 = 4.36 Å and r2 = 2.59 Å | 1.65 r1 = 4.31 Å and r2 = 2.61 Å | 1.2 r1 = 2.73 Å and r2 = 2.28 Å | 1.61 r1 = 2.68 Å and r2 = 1.66 Å |
| Ratio between spacings as indicated in Fig. 2 for epsilon-Fe2O3 (referred to as r1 and r2) | 1.72 r1 = 4.39 Å and r2 = 2.55 Å | 1.72 r1 = 4.39 Å and r2 = 2.55 Å | 1.22 r1 = 2.71 Å and r2 = 2.23 Å | 1.6 r1 = 2.71 Å and r2 = 1.69 Å |
| Ratio between spacings in magnetite (referred to as r1 and r2) | 1.66 r1 = 4.2 Å and r2 = 2.53 Å | 1.66 r1 = 4.2 Å and r2 = 2.53 Å | 1.17 r1 = 2.97 Å and r2 = 2.53 Å | 1.57 r1 = 2.53 Å and r2 = 1.61 Å |
| Angle measured between two sets of reciprocal spacings (degrees) | 71 | 70.5 | 64.7 | 85 |
| Angle between reciprocal lattice directions as indicated in Fig. 2 for epsilon-Fe2O3 | 73 | 73 | 64.1 | 86.4 |
| Angle between reciprocal lattice directions in magnetite | 72.5 | 72.5 | 64.8 | 80 |