Additional Information

Hollow gold nanoshells-incorporated injectable genetically engineered hydrogel for sustained chemo-photothermal therapy of tumor

RuiMei Jin1‡, Jie Yang 1‡, DongHui Zhao1, XiaoLin Hou1, ChaoQing Li1, Wei Chen1, YuanDi Zhao1, 2, ZhongYuan Yin3, * and Bo Liu1, 2, *

1 Britton Chance Center for Biomedical Photonics at Wuhan National Laboratory for Optoelectronics - Hubei Bioinformatics & Molecular Imaging Key Laboratory, Collaborative Innovation Center for Biomedical Engineering, College of Life Science and Technology, Huazhong University of Science and Technology, Wuhan 430074, Hubei, P. R. China

2 Key Laboratory of Biomedical Photonics (HUST), Ministry of Education, Huazhong University of Science and Technology, Wuhan 430074, Hubei, P. R. China

3 Cancer center, Union Hospital, Tongji Medical College, Huazhong University of Science and Technology, Wuhan 430022, Hubei, P. R. China.

* Corresponding author.

Fax: (+) 86 27-8779-2202

E-mail address: yzyunion@163.com (Z.-Y. Yin)

E-mail address: lbyang@mail.hust.edu.cn (B. Liu)

1 These authors contributed equally to this work

Fig. S1. The hydrodynamic sizes of HAuNS, DOX/HAuNS nanoparticles, and PC10A/DOX/HAuNS nanoparticles.

Fig. S2. High resolution SEM image of PC10A/DOX/HAuNS hydrogel.

Fig. S3. SEM images of blank PC10A hydrogel (A), PC10A/DOX hydrogel (B), and PC10A/HAuNS hydrogel (C).

Fig. S4. PC10A/DOX/HAuNS hybrid hydrogel was transferred into a syringe and passed a 26-gauge needle.

Fig. S5. Temperature changes of PC10A/DOX/HAuNS nanogels (PC10A: 0.1% w/w, DOX: 0.8 mg mL-1) irradiated with an 808 nm laser for 9 min under different power densities (0.5, 1.0, 1.5, 2.0, and 2.5 W cm-2). n = 3.

Fig. S6. (A) PC10A/HAuNS hydrogel and PC10A/DOX/HAuNS hydrogel (PC10A: 3% w/w, DOX: 0.8 mg mL-1, HAuNS: 20 μg mL-1) was exposed with an 808 nm laser at a power density of 2.0 W cm-2 for 9 min (B) and cooling down under room temperature (C).

Fig. S7. Standard curve of DOX measured with absorption spectra at 480 nm.

Fig. S8. Photographs of hemolysis ration of water, PBS, PC10A hydrogel, and PC10A/HAuNS hydrogel incubated with RBC for a series of time points (2, 4, and 8 h).