High-Hole-Mobility Metal-Organic Framework as Dopant-Free Hole Transport Layer for Perovskite Solar Cells

Ruonan Wang,a‡ Weikang Yu,a,b‡ Cheng Sun,a‡ Kashi Chiranjeevulu,c Shuguang Deng,d Jiang Wu,e Feng Yan,f Changsi Peng,g Yanhui Lou,*,a Gang Xu,*,c Guifu Zou*,a

a College of Energy, Soochow Institute for Energy and Materials Innovations, and Key Laboratory of Advanced Carbon Materials and Wearable Energy Technologies of Jiangsu Province, Soochow University, Suzhou 215123, China.

b School of Resources Environmental & Chemical Engineering, Nanchang University, 999 Xuefu Avenue, Nanchang 330031, China.

c State Key Laboratory of Structural Chemistry, Fujian Institute of Research on the Structure of Matter, Chinese Academy of Sciences, Fuzhou, Fujian 350002, China.

d School for Engineering of Matter, Transport and Energy, Arizona State University, 551 E. Tyler Mall, Tempe, AZ 85287, USA.

e Institute of Fundamental and Frontier Sciences, University of Electronic Science and Technology of China, Chengdu 610054, P. R. China.

f College of Chemistry, Chemical Engineering and Materials Science, Soochow Universit, Suzhou 215123 (China).

g School of Optoelectronic Science and Engineering and Collaborative Innovation Center of Suzhou Nano Science and Technology, Soochow University, Suzhou, 215006, China.

‡ These three authors contributed equally to the work.

* Email: yhlou@suda.edu.cn; gxu@fjirsm.ac.cn; zouguifu@suda.edu.cn

Content:

Supporting figures

Figure S1. Illustration of the assembly process for the Ni3(HITP)2 film. a) The cleaned ITO substrate; b) The precursor solution for synthesis of Ni3(HITP)2 film; c) After the Ni3(HITP)2 film is formed, lift-down ITO along of the beaker; d) Lift-on the membrane by slowly raising the ITO and e) ITO substrate coated with complete Ni3(HITP)2 film.

Figure S2. EDX mapping of the Ni3(HITP)2 membranes.

Figure S3. XPS spectra of the Ni3(HITP)2 membranes.

Figure S4. AFM images of different thickness of Ni3(HITP)2 membranes.

Figure S5. Photographs of the bare ITO glass and with different thickness of Ni3(HITP)2 membranes.

Figure S6. Steady-state PL spectra of perovskite/ITO based on 20nm, 30nm, 40nm, and 50nm Ni3(HITP)2 film and PEDOT/PSS; Inset: the enlarged steady-state PL spectra of perovskite on the 20nm and 30nm Ni3(HITP)2 film repeated by three times, respectively.

Figure S7. Time-resolved PL spectra of perovskite on the ITO substrate with different thicknesses of Ni3(HITP)2 film and PEDOT/PSS.

Figure S8. AFM images of different thickness of Ni3(HITP)2 membranes. a) Bare ITO glass, b)-e) Corresponding to 20 nm, 30 nm, 40nm and 50 nm Ni3(HITP)2 membranes, respectively.

Figure S9. XRD pattern of perovskite films deposition on different thickness of Ni3(HITP)2 membranes.

Table S1. The average decay lifetimes of the perovskite/ITO with different hole transport layers.

|  | Without | PEDOT/PSS | Ni3(HITP)2 (20 nm) | Ni3(HITP)2 (30 nm) | Ni3(HITP)2 (40 nm) | Ni3(HITP)2 (50 nm) |
| --- | --- | --- | --- | --- | --- | --- |
| Average τ(ns) | 18.14 | 6.17 | 1.89 | 1.18 | 2.82 | 3.02 |